## Slide 1: Optimization of CVD parameters for graphene synthesis through design of experiments
Remi Papon, Christel Pierlot, Subash Sharma, Sachin Maruti Shinde, Golap Kalita, and Masaki Tanemura
Notes compiled 4/24/20, Sean Lai

## Slide 2: Motivations
CVD Process parameters require time consuming experiments + setups to optimize
Use of DOE can help identify contextual importance of experimental parameters
Without DOE 2P experiments needed for P parameters
5 parameters for these experiments: Growth temperature, anneal time, Carbon source mass, Carbon source heating rate, distance from furnace
In this paper, experiments are reduced to two sets of 23 experiments by holding certain parameters constant and comparing experimental sets (16 total experiments)

## Slide 3: Parameter Details
Fixed one parameter at a time: Cu temperature or annealing time
Tested high/low (+, -) values for the other 4 parameters  8 experiments per fixed parameter  16 total experiments
Fixed anneal time at 30 minutes for first set
Fixed temperature at 1070C for second set
Schematic of experimental setup and example heating/cooling temperature profiles

## Slide 4: Results
Most relevant parameters in DOE matrices. + and – refer to higher or lower of two tested values:
DOE1 (fixed t = 30 minutes):
+ Temperature, 1070C
- increasing rate, 1.5C/min
- Mass of C, 5mg
DOE2 (fixed T = 1070C):
+ anneal time, 60 minutes
- increasing rate, 1.2C/min
- growth time, 90 min
+ mass of C, 5mg
Response to bending angles of graphene and ITO OPV cells

## Slide 5: Optimization
Data used to create contour curves to inform further experiments
Optimized parameters by analysis of DOE experiments: 60 minute anneal time, 5mg C source, 1cm distance, 1.4C/min increasing rate, 72 min growth time
Results: 50-130um crystals, and 60mm domain(?)
A 60um single-layer graphene crystal grown using optimized parameters from DOE analysis and associated Raman scpectra

## Slide 6: Questions + Conclusions
DOE can help optimize experimental parameters to good precision while reducing the required number of experiments
High anneal temperatures and long growths on Cu produce high quality + large single crystals
How does DOE address non-linear relationships between parameters and outcomes?
How do the number of required experiments scale if optimizing for two different output parameters?