## Slide 1: C‐Plane Sapphire and Catalyst Confinement Enable Wafer-Scale High-Quality Graphene Growth
Lester F. Lampert, Roman Caudillo, Thomas Lindner, and Jun Jiao

## Slide 2: Research Motivations
Graphene has desirable qualities to the semiconductor industry
Copper (Cu) thin films are widely used to grow graphene on Si substrates
Important parameters
Cu has poor adhesion with SiO2
Cu (111) orientation is shown to have best growth characteristics  C-plane sapphire
Catalyst confinement shown to help control Cu surface characteristics

## Slide 3: Experimental Results: H2 effects
H2:CH4 ratios used: 10:1, 20:1, 30:1, 50:1 69:1
Higher H2 resulted in rougher Cu surface, higher bilayer density
Lower H2 had reduced single-crystal growth and amorphous domains
Bilayer density increased exponentially with H2 levels.

## Slide 4: Experimental Results: Raman analysis
10:1 and 69:1 ratios had best graphene quality -> majority monolayer
high 2D/G peak ratios
2D peak shape (low full-width at half maximum)
69:1 showed high bilayer density

## Slide 5: Experimental Results: Using CC for SiO2 Wafer
Without CC the Cu film is unstable -> voids, delamination
3mm catalyst offset used for experiments
Temperatures used: 770, 780, 790°C
790°C found the have largest Cu grains
Higher temps yielded better quality, but more cracks

## Slide 6: Conclusions/Questions
Tradeoff between high-quality graphene and high bilayer density at high H2::CH4 ratios could warrant further research/optimization
What scales of single crystal monolayer graphene are needed for viability in semiconductor applications?
We use acetylene often in the lab. What are the differences in graphene seeding between CH4 and C2H2?
Possible label mix up on figure 5 of the paper
What is happening to Cu at temperatures > 790°C?
Why do BEOL applications require low temperatures and what range is considered low?
How does H2 increase Cu mobility -> large domains of single crystal C(111), shown in figure 3?
Are there other methods to produce highly uniform Cu(111) films?